## Slide 1
Impedance Spectroscopy
Using the Matlab program
ZfitGUI
Theory and other things may be found in the Macdonal book and here :
https://sites.google.com/site/jeanlucdellis (in the « programmes Matlab » and in the « Spectroscopie d’Impédance» repertories)

## Slide 2
Download the Matlab program ZfitGUI
Z fit GUI
Impédance Z
Fit : search for the best parameters of an Equivalent Circuit
Graphical
User
Interface

## Slide 3
Preambule
If a semi-circle is found in the Z-representation, one may use the parallel model p(R1,C1). It means that when the EC is submitted to a voltage, the current comes from 2 additive contributions. One is dissipative when the other is conservative . If the semi-circle was shifted along the real Z axis, just add a resistor in series to fit the spectrum. In the same vein, note that the series EC
s(p(R1,C1), p(R1,C1)) will give 2 successive semi-circles, less or more overlapped.
If the semi-circle was found in the C-representation, the right EC is the serial Debye model s(R1,C1) with only one current usually attributed to the material
Impedance is a complex number which is frequency dependent as are the related immitances like for instance, the complex capacitance : . The curve is called spectrum as well as . To model these data, one may use equivalent circuit (EC). The spectra have usually one or more semi-circle loops whose analysis allows to separate intrinsic phenomena of those arising from the electrodes, the wires or even the apparatus effects.
polarization and which equilibrium is delayed by the resistor. If the semi-circle was shifted along the real C axis, just add a capacitor in parallel to fit the data. Here also, we may find 2 successive semi-circles but the model would be : p(s(R1,C1), s(R1,C1)) .

## Slide 4
Download simulations and experimantal data
In Internet, search for the google web site « jeanlucdellis », navigate to the « programmes Matlab » repertory to download the files to process as trainings.
Download
Get the function ZfitGUI, the Tutorial and the User Manual

## Slide 5
the Matlab program ZfitGUI adds UIMENUS to a figure
Type ZfitGUI without inputs :

## Slide 6
How to generate simulated Z-data
Click ‘Circuit’ to enter the frequency bounds.
Default : 1 Hz to 106 Hz…
… and to enter the Circuit String. Default string is : s(p(R1, C1), R1).
‘s’ stands for ‘put in series’ and ‘p’ for ‘put in parallel’. These operators must have exactly 2 arguments. The numerals beside the element letters R (resistor) and C (capacitor) are reminders about the amount of parameters they need. L1 (inductor), E2 (CPE), G2, H2 (diffusion impedances) and even user-defined element may be used. Read the User Manual of ZfitGUI to have more details about them.
It is mandatory to enter values for the elements. Enter them as they come in the Circuit String.
Default : 5 104, 10-9, 5 103
Note that ‘Graph’ contains sub-menus

## Slide 7
Click on the « Load Data » uimenu to load Z2Loops in ZfitGUI
Z2Loops – Fitting a simulated Data of a conductive system (A)
Next step is to select the curve, write a Circuit string and feed it with initial values
Before to proceed, clean the figure with the « edit plot » tool (arrow of the menu), then right-click on the preceeding curve and delete it.

## Slide 8
The tools in the bottom of the Result figure are very usefull :
Click on «SelectLine » to process the curve
Click on « Circuit » to enter the Circuit string and the Pinit. As the spectra usually show loops, « s(p(R1,C1),R1) » is a good start because p(R1,C1) defines a semi-circle which can be translated along the real axis with the s( ,R1) operator
Z2Loops – Fitting of a simulated Data of a conductive system (B)
Click on «Fit», then twice on the large loop to fit it and …
… to get the results graphically and in the Result figure:
Try to fit the whole spectrum with s(p(R1,C1), p(R1,C1))
Very usefull : the values in the Value colunm are editable. Change them to get a better initial parameters set.

## Slide 9
Load ‘C2Loops’. One obtains a Z-spectrum looking like the one of a capacitor, lets switch to : ‘Graph, -Ci=f(Cr)’
C2Loops – Fitting of a simulated Data of a dielectric system
It gives a main loop and the beginning of another at HF (checked in using ‘Graph, frequency?’)
When in « C » representation, for dielectric systems, 2 successive loops correspond to 2 Debye relaxations s(R1,C1) in parallel. So here, we will use the Circuit String : p(s(R1,C1), s(R1,C1)) and from the spectrum inspection, we shall start with capacitors 5 10-10 F (at HF) and 15 10-10 F (at LF).
One may examine the Re(Z) = f(ω) curve to get initial values 104.4 Ω (at LF) and 101.8 Ω (at HF) or use « Fit » and a try and error method.
The Initial parameters have little error in the C guesses but anyway, lets try « Fit »

## Slide 10
Circuit1 – Pay attention to low amplitude points
Enter the model string after clicking on the "Circuit" menu and initial (guessed) values
Click on « FIT »
Check the results
Small biases may have important consequences on the fitting success. A good strategy is to check the Re(Z) = f(ω) and the Im(Z) = f(ω) curves. One finds and .
Very useful : with the « edit plot » tool ( ), you may delete any graphic object …
s(R1, p(R1, C1)) is the right Circuit string.
Procedure :
Inpect the spectrum. Here, we find with the tool and the zoom
that the semicircle is translated along the axis of the reals:

## Slide 11
s (p (R1, C1), E2)
Guessed Values obtained from inspection of the graphs
4 Hints :
Zoom the HF
change graph to complex C
use « Graph + Frequency ? »
Remind
Circuit2 – Simulated Data with an CPE
Fit …

## Slide 12
Circuit3 – Simulated Data with low frequency dispersion
Steps (example) :
Firstly, use a simple s(R1, p(R1, C1)) circuit.
Use the « Fit » tool for the HF (fig2). The RC is OK for the HF but it looks like there is anoher relaxation at LF s(p(R1,C1),p(R1,C1)).
The fit on the mid frequencies (fig3) seems enough good.
To go further, a zoom for the LF revealed that the experimental Z came on the real axis with a different slope compared to the RC model in red (fig4) try s(p(R1,C1),p(E2,C1)) using the initial values from fig4 (adding an exponent of 0.01 for the CPE which mimics a ‘dispersive’ resistor)
Fit …
mid frequencies

## Slide 13
Maruse – Experimental Data
Steps (example of corrupted data) :
The experimental HF part of the loop of fig3 (model used : s(R1,C1)) would extrapolate to negative value ! p(C1,s(R1,C1)) with the first C<0 initialized to -1e-9.
fit the mid frequencies (fig4) or remove the outliers from the « Graph » menu (fig5) or search if CPE or diffusion impedances could improve the fitting if interressed in the LF side of the system (= refine the model).

## Slide 14
Panata – Experimental Data
model : s(R1,p(R1,E2))
Khi2 of fit: 2.08e-3
P1 = 1.17e-1
P2 = 6.87e+0
P3 = 1.27e-3
P4 = 7.58e-1
Khi2 is a measure of the distance experimental/model
Because Khi2 depends on the amount N of points taken in the fit, the normalized Khi2/N is displayed in the result figure.
Steps (example of corrupted data) :
Remove the HF outliers (with positive Zi).
Note that there is a small translation of the spectrum of (fig1).
A semi-circle whose the center is located under the real axis can be related to a p(R1,E2) circuit when in Z-representation. Adding the little resistor , one tries s(R1,p(R1,E2))
The initial values are guessed from the Z and the C representations
Fit …

## Slide 15
Legreen – Experimental Data – a difficult case
Using the model s(p(R1,C1),p(R1,C1)) and « Fit » on the mid frequencies gave fig1 with
'model : s(p(R1,C1),p(R1,C1))‘
‘Khi2 of fit: 2.37e-2'
'P1 = 2.18e5‘
'P2 = 2.19e-9'
'P3 = 4.43e5‘
'P4 = 5.97e-9‘
Further investigations leads to use a model with a Finite Length Warburg with SHORT Circuit “G2” and a much better result altought using the same amount of parameters (4) :
'model : p(p(R1,C1),G2)‘
‘Khi2 of fit: 9.43e-4'
'P1 = 7.89e5'
'P2 = 1.29e-9'
'P3 = 3.55e-8'
'P4 = 1.55e-1'
mid frequencies
mid frequencies
In M representation, the result is very good except at the high frequencies where there is an abnormal behavior with Mr decreasing in the experimental data. Maybe due to the apparatus …

## Slide 16
Ambiguïty of the models
The blue curve named « circle123 » are very similar to the experimental data processed above with a Finite Length Warburg with SHORT Circuit :
p(p(R1,C1),G2)
Try to find the parameters giving the red line which at first glance seems statisfying.
However, watching the real Z-part gave the figure 2 where one can state a gap at the high frequencies. It is also visible when using the M-representation (figure 3).
Read the next slide to know from where circle123 comes…

## Slide 17
Producing simulated data
Using the model p(R1,C1) in « circuit », we produced circles 1, 2 and 3. The parameters were successivly :
    p(1) = 1e4 then 2e4 and 3e4
p(2) = 1e-9 then 2e-9 and 3e-9
To produce the spectrum of these impedances all put in series « circle123 », the model was :
s(p(R1,C1),p(R1,C1))
with :
1e4,1e-9,2e4,2e-9,3e4,3e-9
[At a fixed frequency , the point of the resulting spectrum is
Beware, the figure shows a special case where the points are aligned but usually they are not]
Try this model on the Legreen data …